## Slide 1: Automatic Zoning Preliminary Results July 22, 2014

## Slide 3
Three methods:
Pure geometrical: minimize distance of each point in a zone from its centroid
State variables: Use state variables at completion of forging
Point tracking : Use state variables at all times during the forging; in progress
To be done:
Complete Item 3
Test all options with different numbers of zones and different initial guesses

## Slide 4
Pure geometrical: minimize distance of each point in a zone from its centroid
Note – Tested with different initial guesses for the centroids and all converge to almost the same solution.
I thought this would be symmetric (top-bottom) – I need to make sure there are no errors. This may be because the mesh is not symmetric and I am using the element centroids as the point locations. Weighting by the area of the element may make it more symmetric.
Zone 7 are the centroid locations.

## Slide 5
State variables: Use state variables at completion of forging;
used only temperature and strain; but the program is general and can include any number of variables, each with its own weighting factor.
All state variables normalized to lie between 0 and 1.

## Slide 6
State variables: Use state variables at completion of forging;
used only temperature; Looks similar to temperature contours

## Slide 7
State variables: Use state variables at completion of forging;
used only strain; Looks similar to strain contours

## Slide 8
Temperature and Strain
Strain
Temperature
Comparison of using different state variables

## Slide 9
The zoning based on any single state variable looks like the contours of that variable from DEFORM.
We can combine all the state variables, each with its own weighting factor, into a new user defined variable in DEFORM, and plot the contours of the user defined variable to help us define how the forging should be zoned.
Possible zoning based on temperature and strain.
I can try to automate this by defining the geometrical centroids of the zones and then gradually expanding a rectangle around this centroid until a specified fraction of its area runs into another zone